NITROCELLULOSE SOLUTION

STANDARD GRADES

| EURO NORM | MIDAD REFERENCE | VISCOCITY INDEX ASTMD 1343 | NITROGEN CONTENT | HIGHEST PERCENTAGE OF NC IN THE SOLUTION 70±2 SOLIDS |
| --- | --- | --- | --- | --- |
|  |  |  | HIGH |  |
| 4 E 5 E 6 E 7 E 8 E 9 E 12 E 22 E 23 E 25 E 27 E 32 E | MH 800 MH 300 MH 120 MH 80 MH 35 MH 20 MH 5 MH 3/4 MH 1/2 MH 3/8 MH1/4 MH 1/8 | 600 - 1000 SEC 250 - 350 SEC 100 - 140 SEC 80 - 120 SEC 30 - 40 SEC 15 - 20 SEC 5 – 6 SEC 3/4 SEC 1/2 SEC 3/8 SEC 1/4 SEC 1/8 SEC | 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 11.7 – 12.2 | 12 % 15 % 18 % 20 % 25 % 30 % 35 % 40 % 50 % 50 % 50 % 55 % |
| EURO NORM | MIDAD REFERENCE | VISCOCITY INDEX ASTMD 1343 | NITROGEN CONTENT | HIGHEST PERCENTAGE OF NC IN THE SOLUTION 70±2 SOLIDS |
| 12 M 22 M 27 M | MM 5 MM 1/2 MM 1/4 | 5 – 6 SEC 1/2 SEC 1/4 SEC | MEDIUM | 35 % 50 % 50 % |
|  |  |  | 11.2 – 11.7 11.2 – 11.7 11.2 – 11.7 |  |
| 15 A 23 A 27 A 30 A | ML 5 ML 1/2 ML 1/4 ML 1/8 | 5 -6 SEC 1/2 SEC 1/4 SEC 1/8 SEC | LOW | 35 % 50 % 50 % 55 % |
|  |  |  | 10.7 – 11.2 10.7 – 11.2 10.7 – 11.2 10.7 – 11.2 |  |

① Nitrocellulose percentage in the solution depends on the choice of solvents mix by the clients as it affects the viscosity of the solution ( this is explained in the viscosity of the solution below ).

② Final viscosity of the solution is determined according to clients requirements of the nitrocellulose percentage, grade, and the solvents required, and will be provided to the client after implementing the formula provided in the lab.

③ The above table contains the main grades of nitrocellulose, and other grades can be provided according to clients requests.

Viscosity of the solution :

The viscosity depends mainly on the Solvents required by the customer, as different solvent combinations and NC nitrogen content will result in different viscosities and will affect the dissolution process and the final viscosity of the solution.

There are three groups of solvents which will effect directly the dissolution process and the final viscosity of the solution:

1- Active solvents:

These solvent are very effective in dissolving nitrocellulose at room temperature and will help in giving lower viscosities and will help in increasing the NC content of the solution.

- Ketones           :  acetone, MEK, MIBK,…

- Esters               :  ethyl acetate, butyl acetate, methoxy propyl acetate ,…

- Alcohols             : Ethanol ( only with low nitrogen content nitrocellulose )

- Glycol ethers  : methoxy glycol ether, ethyl glycol ether,…

2- Inactive solvents :

These solvents are not capable of dissolving nitrocellulose on their own and need to be activated with active solvents.

- Alcohols  : ethanol, isopropanol, butanol,….

- Ethers      : diethyl ether , dimethyl ether, tetrahydrofuran, dioxane,….

3- Non- solvents :

These solvents are not capable of dissolving nitrocellulose neither on their own nor with mixing them with active solvents, and they are solely used as extenders or diluents for the solution.

- Alipahatic hydrocarbons   : methane, ethane, propane, hexane, heptane,…

- Aromatic hydrocarbons    : toluene, xylene, benzene,…

Compatibility:

Nitrocellulose is compatible with almost all resins used in the coatings industry, as it is seldom used alone as a film former, since the optimum properties are obtained from combining it with other resins.

The main resins usually used in combination with nitrocellulose are:

Alkyd, ketone, polyvinyl Acetate, acrylic, maleic, amine, fumaric, phenolic, epoxy, polyamide,  polyester, vinyl.

Which are incorporated with the NC solution and will give the required characteristics of the final product, mainly: Flexibility and Elongation, Hardness, Solubility, Viscosity, Solid content, Adhesion, Gloss and Thermopalsticity.